## Slide 1: Modeling X-ray photoelectron diffraction forcing/accelerating convergence
Photo Electron Diffraction
Shin Yasuda1, Mariko Terao−Dunseath2, Kevin Dunseath2, Sylvain Tricot1, Didier Sébilleau1
1Department of Material and nanoscience, Institute of Physics, University of Rennes, France
2Department of molecular physics, Institute of Physics, University of Rennes, France
1. Introduction
3.905 Å
[100]
[010]
[001]
Sr
Ti
O
3.905 Å
[100]
[010]
[001]
Sr
Ti
O
2. Theory & Method
diverges if
In MsSpec [1] calculating the intensity:
Idea [2]:
Mix and with parameter ω:
The calculation is as heavy as MI (Matrix Inversion).
[1] D. Sébilleau et al., Comput. Phys. Commun. 182, 2567-2579 (2001). [2] A. Takatsu, et al., Phys. Chem. Chem. 24, 5658–5668 (2022).
We hope for someparameter:
For 1000 atoms, around 3 weeks !
3. Computational details 4. Results & Discussion
X-ray
PED calculation for LaAlO3 (Mohamed Zanouni, Faculty of Sciences, Tangiers, Morocco)
Motivation from this divergence !
Where it comes from ?
How to cure it ?
O Emitter
1729 atoms
Ti Emitter
X-ray
: Sr
: Ti
: O
1920 atoms
1: Compute the cross section for an emitter at each plane
2: Sum all signals → interference between the planes
STO cluster with Ti emitter
STO cluster with O emitter
Trick
Our Method ~ Atomic chain approximation ~
5. Conclusion & Perspectives
Photoelectron kinetic energy: 1019 eV (Ti), 948 eV (O)
Exchange and correlation potential: Hedin-Lundqvist complex
Path filtering: 30 of Forward Filtering (FF30)
: {Sr, Ti, O} = {29, 29, 29}
Scattering order = 6
We have found out divergence effect on an atomic chain. We demonstrated our methodology simulating theta scans for STO based on atomic chains. More perovskites are to be tested (CTO, BTO,…etc., experimental data are available at the IPR).
Strontium Titanium Oxide (STO) is of great importance:
Ferroelectricity
: Sr
: Ti
: O
Ⅰ
Perovskite
Ⅱ
Ⅲ
Simulation and experiment
Ⅰ
Theory in MsSpec
Ⅱ
z
Ⅰ
Ⅱ
Ⅰ
Ⅱ
*
: Free propagator
: T-matrix
z
Divergence effect never shows up with
Good agreement with experiment
Fine peaks are reproduced by ~ 1000 atoms
Same fruits as Ti emitter !
Parameters
[3]
k: Photoelectron kinetic energy
a: Muffin-tin radius
・1019 eV (Ti) -> {19, 15, 13}
・948 eV (O) -> {18, 15, 12}
[3] S. Tricot, et al., J. Electron Spectrosc. Relat. Phenom. 256, 147176 (2022).
Renormalized
Not Renormalized
Not Renormalized
Renormalized
Notes: I have to change the logo to newSTOの名前、Oがない。
Normal vecotrの色
平均自由行程で1000個ほしい
鎖の前方散乱や香蘭散乱に発散の原因があるとにらんでいる
Clusterの図のreference
Lmax見積もり
Scattering を変えて収束性を確かめる
100個のクラスターの図もやる